## Slide 1: HORN FORMATION ON MULTIPHASE DIFFUSION PATHS
John Morral and Yunzhi Wang
Department of Materials Science and Engineering
The Ohio State University
Columbus, Ohio 43210
NIST Diffusion Workshop
February 7-8, 2006

## Slide 2: OUTLINE
Horn definition
Importance of horns
Seminal paper
Theoretical basis for single Horns
Numerical example
Horns in Ni-Cr-Al
Conclusions

## Slide 3: Horn definition “Sharp deviations (singularities) in zigzag diffusion paths”
20
25
30
10
15
20
25
30
Al (at %)
Cr
(at %)

’


0
15
5
10
Hopfe, William D. and J. E. Morral. Acta Metall. et Mater. 42 (1994) 3887-3894.
horns on a diffusion path
(variable [D])
zigzag diffusion path (constant [D])

## Slide 4
Why Horns are important They can lead to the formation of brittle intermetallic compounds at bond interfaces
 layer

## Slide 5
1994 Phase Transformation Meeting

## Slide 6
DICTRA Finite Difference Simulation of a  Diffusion Couple
    Anders Engstrom, J.E. Morral and John Ågren. Acta Mater. 45 (1997) 1189-1199.

## Slide 7: Seminal paper on Horns

## Slide 8: Types of Horns
“Double Horn”
DICTRA simulation
“Single Horn”
Analytical, Perturbation
method solution

## Slide 9: Deviation from the linear zigzag path that isn’t a horn
Exceptional Case
Numerical simulation

## Slide 10: Comparison of two numerical simulations
M. Schwind, T. Helander,
J. Agren, Scripta Mater. 44
(2001) 415-421
Single Horn
Linear variation
of D with concentration
No Horn
Parabolic variation
Of D with concentration

## Slide 11
M. Schwind, T. Helander,
J. Agren, Scripta Mater. 44
(2001) 415-421
Single Horn
Linear variation
of D with concentration
No Horn
Parabolic variation
Of D with concentration
Path with no horn is smooth when
the composition jump at the initial interface is removed

## Slide 12: Theoretical Basis for Single Horns The continuity equation is the key
dx

## Slide 13: Theoretical Basis for Single Horns
Predicted by theory
Not predicted by theory

## Slide 14
Numerical example of the of the A-B-C system
(d)
Flux profile
Concentration
profile
K. Wu, J.E. Morral and Y. Wang, submitted to Acta Mater, Jan. 2006

## Slide 15: DICTRA Simulations of Ni-Cr-Al +  diffusion paths
“On diffusion paths with ‘horns’…” H. Yang, J.E. Morral, Y. Wang, Acta Mater. 53 (2005) 3775-3781

## Slide 16: DICTRA simulations of Ni-Cr-Al +  diffusion couples
Simulations by Dr. Ximiao Pan 2006
Diffusion Path
Flux Profiles

## Slide 17: Numerical simulations of Ni-Cr-Al +  diffusion paths
Simulations by Dr. Ximiao Pan 2006

## Slide 18: “New model”simulations of Ni-Cr-Al +  diffusion paths
Simulations by Henrik Larsson - 2006

## Slide 19: CONCLUSIONS
Only single horns are predicted by the diffusion equation for multiphase diffusion couples if the diffusivity varies with composition.
The exception is that no horns will form if the diffusivity doesn’t vary at x = 0.
Double horns occur in DICTRA simulations, but their origin is unknown.

## Slide 20
THE END